## Slide 1: Comparison of Soviet- era and modern multi-digestion rock geochemical and mineralogical methods for vectoring toward mineralising systems Charlie Moon

## Slide 3: Mining Area C
Originally Mt Goldsworthy JV (Consolidated Gold Fields (33%) Utah Cyprus 1964
Now BHP 85%, Mitsui 8%, Itochu 7%
CGF exited 1977
First production 2003
Current production 62 Mt, costs 1-2nd quartile
Royalty $A60-80 M (2022) previously to Iluka (CGF residue)

## Slide 4: South Deep (30-50 Moz)

## Slide 5: Pakistan

## Slide 6: Examples of Detail Bagrot HMC
Arsenopyrite
Chalcopyrite

## Slide 7: Waziristan

## Slide 8: Former Soviet Union

## Slide 9: Soviet Union
Kounrad- Kazakhstan

## Slide 13: Cu Pb Zn Mo Ag As Co Ni Cr V Mn Ti Zr Sc Li BeP Ba W Sn Bi Sb Ge Y Au DC arc spectrometry + thin section (point counted)

## Slide 15: Distance from Yubileinoe centre

## Slide 16: Distance from Yubileinoe centre normalised
Cun *Aun*Mon
Cun
Cu
Cun *Agn*Bin

## Slide 17
%

## Slide 18: Distance from Yubileinoe centre

## Slide 20
Total
Granitoid
Volcanic

## Slide 22: What has changed since 1990s?

## Slide 23: pXRF 2011 Rovaniemi demonstration

## Slide 24: 2020s Analytical Methods
Granites
Acme XRF and CSM ICP-MS
SiO2 TiO2 Al2O3 Fe2O3 MnO MgO CaO Na2O K2O P2O5 XRF beads (LOI Total)
Ba Cr Cs Cu Ga Ni Pb Rb Sc Sr Th U V Y Zn Zr. (La Sn Nb As) XRF pellets
Ce Dy Er Eu Gd Ho La Lu Nb Nd Pr Sm Sn Ta Tm W Yb Zr Ge In Li Pb Zn As Bi Sb Tl Be
4 acid (HF) digestion ICP-MS +aqua regia
Cl F KOH fusion Ion Chromatography DL 25ppm; OL 2% Loughrea ALS
B Na2O2 ICPMS glass free Vancouver ALS
Elvans (Dykes)
ALS majors mostly ICP-ES Li metaborate fusion, some XRF, traces fusion + 4 acid + aqua regia + F Ion Chromatography
Initial +OL Sn pXRF
Additional cost B F Cl ~50% ϵ 180
QA/QC 10%

## Slide 25: RS12 width 2cm
Quartz | 19.875
K-Feldspar | 29.026
Plagioclase | 23.536
Biotite/Zinnwaldite | .473
Muscovite/Lepidolite | 8.296
Chlorite | 0.029
Tourmaline (Schorl) | 1.529
Kaolinite | 0.073
Topaz | 1.013
Al silicates/Elbaite | 0.237
Zircon | 0.001
Petalite/Beryl | 14.766
Amblygonite-Montebrasite | 0.001
Columbite | 0.005
Uraninite | 0.000
Apatite | 0.131
Fluorite | 0.001
Others | 0.009
Volume %
Automated Mineralogy QEMSCA, MLA, LA-ICPMS

## Slide 26: Critical Minerals

## Slide 28: New Airborne Survey
Datasource: www.tellusgb.ac.uk
200m X 80 m

## Slide 29
Roskear A lode
South Crofty
~2% Sn
Deakin et al., 1995
Main phase lode Pryces Lode
Tourmaline
Veins
Crosscourses
Sheeted vein greisen
Main Styles of Metallic Mineralisation
Skarns

## Slide 30: Rock Geochemistry
Manning et al., 1996
Bromley et al., 1989

## Slide 31
Principal components analysis (PCA)
Increasingly evolved granites?
Distinct G5 granite
PCA comparison shows:
  Clear geochemical evolution trend for G1-G4 granites
  Distinct G5 granite region
  Samples in Simons et al. (2016) classification requiring potential reinterpretation
NB: Meldon Aplite (G5) sample removed from these results

## Slide 32
Unsupervised machine learning (k-means clustering method) on transformed data
8-cluster solution plot
Tregonning G5 Topaz and aplites
St. Austell G5 Topaz
Land’s End G3 granites
St. Austell G4 granites
Dartmoor G3 granites
Scilly G1 granites
Carnmenellis and Bodmin G1 granites
G2 granites
8-cluster solution plot shows the detailed subdivisions of the granites by type and location quite well suggested from Gap Statistic in k-means clustering analysis

## Slide 33
Cluster determination from hclust manhattan distances in a dendrogram
Cluster 3 = G5 granite
Cluster 1 = G2 & G4 granites, with some G1 & G3 granites (i.e., more evolved granites)
Cluster 2 = G1 & G3 granites (i.e., less evolved granites)
Where do interpreted G1 and G3 granite samples come from that sit in hclust method cluster 1?
(i.e., samples that may be more evolved than previously interpreted)
Distance cutoff to distinguish 8 clusters
Distance cutoff to distinguish 3 clusters

## Slide 34
Hemerdon
Wheal Vor
Cornish Tin
United Downs

## Slide 35: Conclusions from Arbavere
Moving Forward: coherent Baltics
Archive data need digitising and web release
New drilling encouraging
Thanks to organisers

## Slide 36: Granite Conclusions
Multivariate methods confirm Simons et al classification with minor tweaks
Very strong correlation of F and Li-W-Ta in G4/5
G2 granites have lower but significant F
B enriched in G2, G4 (strongly) but not G5
F but not B enriched in lamprophyres
Cl depleted in early and altered granites
Sn not enriched in early granites: Sn mineralisation formed by leaching by Cl from micas or rutile by hydrothermal fluid Or concentrated in elvans then leached by greisenisation (Cl). Weak Sn in G5
F, B and lesser extent Cl aid in granite classification

## Slide 37: South Africa
Schlüter 2006

## Slide 38: Rondom

## Slide 39
Resource 10.9 Mt at 0.104 % U3O8 at 80-130 $/kg
25 m centres 100-200 m depth, percussion
400 m centres to define geology
Esso Minerals ~860,000 m drilling, R20.6 M

## Slide 40: Pöhla Erzgebirge First Tin plc

## Slide 41: Composite soils, Sn ppm, wdXRF and pXRF, 5360 samples

## Slide 42: Treliver Minerals (2013-5 drilling)
Fault
Dh